## Slide 1
High-Power and Ultra-Fast Photodiodes at THz Regime
Speaker: Prof. Jin-Wei Shi

## Slide 2
National Central University

## Slide 3
National Central University
Prof. C.-B Huang
Notes: My name is Jhih Min Wun. I come from NCU which locate at north Taiwan.
I want to thanks the Prof. C.-B Huang and his termroom in NTHU.

## Slide 4
Outline
Introduction
Working Principle of NBUTC-PD
High-Power and Ultrafast Modulation Characteristic
Applications for MMW Over Fiber Communication
Conclusion

## Slide 5: RF Spectrum Famine is happening
Jonathan Wells “Fast Than Fiber: The Future of Multi–Gb/s Wireless,” IEEE Microwave Magazine, pp.104–112, May 2009.
MMW band can rescue us from famine of RF spectrum
RF Spectrum Famine

## Slide 6: How to obtain more bandwidth ?
Tadao Nagatsuma Ho-Jin Song, and Yuichi Kado,"Challenges for Ultrahigh-Speed Wireless Communications Using Terahertz Waves,"Terahertz Science and Technology,Vol.3, No.2, June 2010

## Slide 7
Why we need optical fiber for wireless ?
Vincent J. Urick, John F. Diehl, Joseph M. Singley, Christopher E. Sunderman, and Keith J. Williams “Long-Reach Analog Photonics for Military Applications” Optics and Photonics News, Vol. 25, Issue 10, pp. 36-43 (2014)
The loss of coaxial cable in Sub-THz frequency regime is much higher than that of optical fiber
103~104 times
Notes: The loss of coaxial cable in Sub-THz frequency regime is much higher than that of optical fiber

## Slide 8: Sub-THz PD…..
Tadao Nagatsuma Ho-Jin Song, and Yuichi Kado,"Challenges for Ultrahigh-Speed Wireless Communications Using Terahertz Waves,"Terahertz Science and Technology,Vol.3, No.2, June 2010

## Slide 9
S. Koenig, D. Lopez-Diaz, J. Antes, “Wireless sub-THz communication system with high data rate.” Nature Photonics 7, 977- 981 (2013), October, 2013
Why we need high-power sub-THz photo-diode ?
High-power Photodiode
The sub-THz electrical amplifier is not ready yet
We need PD which can deliver high power for long distance wireless links!
Notes: The most important application is Radio over fiber communications systems, where the combination
of electronics and photonics offers higher performance, lower cost and greater functionality.
But the sub-Thz amplifier may not be available.
So The High-power photodiode (PD) are the key components for long distance wireless links.

## Slide 10
110 to 170 GHz
DC to 110 GHz
Photonic Sub-THz Measurement System
Bulky and needs several sets for different bands !
Any solution ?? (single set from dc to ~300 GHz)
DC to 200GHz
Notes: Another application is photonic sub-THz measurement system . As you see, the equipments are Bulky and needs several sets for different bands .
So we want to Use a single Ultra-fast PD to replace bulky MMW-multiplier (NA extender).(倍頻器)

## Slide 11
Photonic Sub-THz Measurement System
Photonic solution can cover
DC to 200GHz !
T. Nagatsuma, M. Shinagawa, N. Sahri, A. Sasaki, Y. Royter, and A. Hirata, “1.55-mm Photonic Systems for Microwave and
Millimeter-Wave Measurement,” IEEE Trans. Microwave Theory Tech., vol. 49, pp. 1831-1839, 2001.
Notes: Photonic solution can cover DC to 200GHz !
In this figure, it can be use high power PD converter optical signal to MMW electrical signal.

## Slide 12
Some Reported Solution-
Uni-Traveling Carrier Photodiode
* H. Ito, S. Kodama, Y. Muramoto, T. Furuta, T. Nagatsuma, T. Ishibashi, “High-Speed and High-Output InP-InGaAs Unitraveling-Carrier Photodiodes,” IEEE J. of Sel. Topics in Quantum Electronics, vol. 10, pp.709-727, Jul./Aug., 2004
CB
VB
Anode
Cathode
Absorption layer
( intrinsic)
Pin PD
CB
VB
Anode
Cathode
Absorption layer
( P-doping)
UTC-PD*
Diffusion block
Charge Storage
Electron Dominated Space-Charge Screening Effect !!
Hole Dominated Space-Charge Screening Effect !!
Jmax ≈ (Vbias+ø)εVcarriers / D2
Vhole << Velectron
Jmax UTC >> Jmax pin

## Slide 13: Limited Power from Sub-THz PD…..
Bad :Less than 1mW at ~300 GHz regime
Good: Lossless optical interconnect
How to get more power (> 1mW) in sub-THz regime ?
Goutam Chattopadhyay, "Technology, Capabilities, and Performance of Low Power Terahertz Sources", IEEE TRANSACTIONS ON TERAHERTZ SCIENCE AND TECHNOLOGY, VOL. 1, NO. 1, SEPTEMBER 2011
Bandwidth can’t cover from DC
Output power can up to 1.23mW
by dual UTC-PD at 300 GHz
Notes: Here show several different kinds of THz generation techniques.
As you see, the UTC-PD photomixers can not offer a high such power compare with another techniques such as frequency multiplier.
But the most attractive advantage by use of photomixers is that we can have almost lossless optical interconnect by use of optical fiber.
But anyway , we still need more power to relays the communication in Sub-THz regime.

## Slide 14
Outline
Introduction
Working Principle of NBUTC-PD
High-Power and Ultrafast Modulation Characteristic
Applications for MMW Over Fiber Communication
Conclusion

## Slide 15
Why UTC-PDs Saturate?
(Field Screening)
(Space Charge Screening)
P
i
N
R(Load)
+
-
Vbias
+
-
Veff
Veff :minimum reverse bias voltage during dynamic operation
Vbias :external bias voltage
Jmax :maximum output photocurrent
A :active area
Vbi :built-in potential
R :load resistance
F :fRC roll-off factor
Ec :critical field
Ve : over-shoot drift-velocity
e :dielectric constant
Ddep :depletion layer thickness
Ddep

## Slide 16
Case I:fT>>f3dB (Not sub-THz regime)
(Field Screening)
(Space Charge Screening)
(3)
(Thermal Degradation/Failure)
Minor
High-bias and good heat-sinking is necessary for high power

## Slide 17
Case I: fT>>f3dB
(State-of-the-art High-Power Performance at 15 GHz)
Zhi Li, Yang Fu, Huapu Pan, Andreas Beling, Joe C. Campbell, “Photodiode with 0.75 W RF Output Power at 15 GHz”, ECOC 2011
180mA, 15GHz, 2700mA-GHz under 10oC
But how about Sub-THz regime?

## Slide 18
Case II:fT~f3dB (Sub-THz Regime)
(Field Screening)
(Space Charge Screening)
(3)
(Thermal Degradation/Failure)
Serious issue!!
You need a thin UTC-PD to attain sub-THz transient time
Substrate
N
I
P
Substrate
N
I
P

## Slide 19
Case II:fT~f3dB (Sub-THz Regime)
(Field Screening)
(Space Charge Screening)
(3)
(Thermal Degradation/Failure)
Serious issue!!
You need a thin UTC-PD to attain sub-THz transient time
Also, you need a small size to sustain a sub-THz RC-limited bandwidth
Substrate
N
I
P
Substrate
N
I
P
Device Heating

## Slide 20
Miniaturized PD: Heat is the killer !!
(Field Screening)
(Space Charge Screening)
(Thermal Degradation/Failure)
500K
300K
Fawcett, W. and G. Hill, Electron. Lett 11, 4 (1975) 80-81.
Serious Degradation on Overshoot Drift Velocity!
Substrate
N
I
P
Device Heating

## Slide 21
Sub-THz regime: High-Bias Works ?
H. Ito, T. Furuta, S. Kodama and T. Ishibashi,"InP/lnGaAs uni-travelling-carrier photodiode with 310GHz bandwidth", ELECTRONICS LETTERS 12th October 2000 Vol. 36 No. 21
H. Ito, T. Furuta, F. Nakajima, K. Yoshino and T. Ishibashi,"Photonic Generation of Continuous THz Wave Using Uni-Traveling-Carrier Photodiode", JOURNAL OF LIGHTWAVE TECHNOLOGY, VOL. 23, NO. 12, DECEMBER 2005
~0.7V for Best Speed Performance
Best Speed Performance for Maximum output power
Increasing Vbias doesn’t work (Intervalley scattering/Heat issue !!)
A small optimum Vbias (External circuit Saturation effect)
Pulse Measurement(No heating) Under 12.5Load
CW Measurement (Heating)
External saturation effect ?

## Slide 22
How to Further Increase Power in Sub-THz Regime?
(Field Screening)
(Space Charge Screening)
(3)
(Thermal Degradation/Failure)
Material
Limited by fRC
Possible!
How to increase Veff in the same Thickness (Ddep) without seriously sacrificing Ve (less heating)??
Let Near-ballistic transport happens in the higher Vbias regime !!

## Slide 23
Our Solution: The NBUTC-PD
Charge layer
Velocity overshoot
Low field in the collector Near Ballistic Transport(~Ve)
High Veff (External bias) Minimize the external screening
effect (But thermal becomes an issue)
Collector
T. Ishibashi and Y. Yamauchi, “A possible near-ballistic collection in an AlGaAs/GaAs HBT with a modified collector structure,” IEEE Trans. Electron Devices, vol. 35, no. 4, pp. 401–404, Apr. 1988.
(20nm)
(120nm)
+
-
Veff
NBUTC
UTC
Lower field in the collector
180KV/cm
120KV/cm
Electrical field simulation
-1.5V

## Slide 24
Another Solution: n-charge layer
at B-C junction
Nearly zero electric field under high current operation!
N-doping:
7 nm,
8.3×1017cm-3
N-charge: To smartly re-distribute the E-field under low bias….
The screening of E-field at AC junction can be minimize!

## Slide 25
Outline
Introduction
Working Principle of NBUTC-PD
High-Power and Ultrafast Modulation Characteristic
Applications for MMW Over Fiber Communication
Conclusion

## Slide 26
The breakthrough of NBUTC-PD:
Geometrical Structure of PD array
Optical MMW Source
Good Heat-Sinking for Sub-THz Operation

## Slide 27: Combined Several Devices: Traveling- Wave PD (TWPD)
Drawback
3dB photo-generated MMW power is sacrificed Dummy Load
Bragg cut-off limited bandwidth Periodic Structure
V0
V1
V2
VN
The net bandwidth is limited by Single PD
Transmission Loss limited bandwidth Major Bandwidth Limitation
How can we overcome
these drawbacks ?
Dummy Load

## Slide 28: Our Solution: Cascade NBUTC-PD
Series of several high-speed PDs
A thin depletion layer (Short carrier drift-time) with a released RC-bandwidth !!
Dummy load and complex E-O design are both not necessary !! (50W load)
RLoad
Capacitance equal to….
Active area
125μm
Itoatal
RLoad
Short carrier drift time !!

## Slide 29: How about high-power performance of cascade PD?
 Although current can’t increase as parallel (TWPD), we can increase size of single-PD for the desired bandwidth to enhance saturation current due to reduction of capacitance.
Cascade Structure:
Itoatal
RLoad
D1
D2
DN
Vbias
 Although Vbias ,Total area thermal problem ~
Will the increase of series resistance be a issue? R nR ?
<
Improve RC-limited bandwidth
by use of cascade structure !!
(nR+50)*C/n
(R+50)*C

## Slide 30
Record high saturation current-bandwidth product (7500mA-GHz, 91GHz) under a 50W load.
Power Performance
Akihiko Hirata, Hiroyuki Takahashi, Ryoichi Yamaguchi, Toshihiko Kosugi,Koichi Murata, Tadao Nagatsuma, Naoya Kukutsu, andYuichi Kado,
“Transmission Characteristics of 120-GHz-BandWireless Link Using Radio-on-Fiber Technologies,” JOURNAL OF LIGHTWAVE TECHNOLOGY, VOL. 26, NO. 15, AUGUST 1, 2008
Measured Saturation Current-Bandwidth Product is record high as “7500mA-GHz” (100GHz, 75mA)
The Output Power Performance of our
2-Cascade-NBUTC-PD is superior to
UTC-PD+HEMT Amplifier Module!!

## Slide 31
 | Bandwidth (GHz) | Saturation current & Bandwidth Product (mA*GHz)
Parallel-fed TWPD (p-i-n PD) [1] | 80 | 1760mA۰GHz
Parallel-fed TWPD (UTC-PD) [2] | 17 | 1938mA۰GHz
Single UTC-PD [3] | 170 | 2380mA-GHz
Single CCUTC-PD [4] | 50 | 2500mA.GHz
Cascade NBUTC-PD [this work] | 100 | 7500 mA۰GHz
Benchmark for High Power PD
A. Beling, J. C. Campbell, H.-G. Bach, G. G. Mekonnen, and D. Schmidt, “Parallel-Fed Traveling Wave Photodetector for >100-GHz Applications,” J. of Lightwave Technol., vol. 26, pp. 16-20, Jan., 2008
A. Beling, H. Chen, H. Pan, and J. C. Campbell, “High-Power Monolithically Integrated Traveling Wave Photodiode Array,” IEEE Photon. Technol. Lett., vol. 21, Dec., pp.1813-1815, 2009.
3. H. Ito, T. Furuta, F. Nakajima, K. Yoshino, T. Ishibashi, “Photonic generation of continuous THz wave using uni-traveling-carrier photodiode,” J. of Lightwave Technol., vol. 23, pp. 4016-4021, Dec., 2005.
4. N. Li, X. Li, S. Demiguel, X. Zheng, J. C. Campbell, D. A. Tulchinsky, K. J. Williams, T. D. Isshiki, G. S. Kinsey, and R. Sudharsansan, “High-Saturation-Current Charge-Compensated InGaAs-InP Uni-Traveling-Carrier Photodiode,” IEEE Photon. Technol. Lett., vol. 16, Mar., pp.864-866, 2004.

## Slide 32
The breakthrough of NBUTC-PD:
Geometrical Structure of PD array
Optical MMW Source
Good Heat-Sinking for Sub-THz Operation

## Slide 33
Akihiko Hirata, Mitsuru Harada, and Tadao Nagatsuma,"120-GHz Wireless Link Using Photonic Techniques for Generation, Modulation, and Emission of Millimeter-Wave Signals,"J. of Lightwave Technol., vol. 21, pp. 2145–2153 ,2003.
Why we need shorter pulse?
Modulation depth ↑
Enhance power ↑
But why?
Notes: In the same photocurrents ,the different modulation depth will have different transfer efficiency for RF Signal.
So we need shorter pulse to get high modulation depth and Enhance power .
The figure shows the Shorter Pulse Provide Higher MMW Power.

## Slide 34
MMW spectral power enhancements
Theoretically enhancement “6dB”
Each pair of two-tone contributes to MMW power
F.-M. Kuo, J.-W. Shi, H.-C. Chiang, H.-P. Chuang, H.-K. Chiou, C.-L. Pan, N.-W. Chen, H.-J. Tsai, and C.-B. Huang, “R Spectral Power Enhancement in a 100-GHz Photonic Millimeter-Wave Generator Enabled by Spectral Line-by-Line Pulse Shaping .” IEEE Photonics Journal,Vol.2, Issue 5,pp.719-729 ,Oct ,2010
Notes: The figure shows the optical field amplitudes for the time-domain sinusoid and pulse.
As can be see, Each pair of two-tone contributes to MMW power .
Theoretically[͵θiəˋrɛtɪk!ɪ] enhancement power is 6dB.

## Slide 35: Summarize the advantages of short pulse
2. High modulation depth→Enhancement power ↑
1. Reduce thermal effect for photodiode
Sinusiodal Singal
Shorter Pulse
Improvement :
Duty Cycle↓
Notes: So if we use shorter pulse ,we have two important Improvement .
Because the smaller duty cycle, we can Reduce thermal effect .
And by use shorter pulse, we also have High modulation depth to obtain more Enhancement power .

## Slide 36: Adaptive Photonic MMW Source for Access Network
Generate 1-ps optical pulse train (~400 GHz rept. rate) for higher MMW power!!
Indepently Manipulate Phase and Amplitude of each comb line!!

## Slide 37
Line-by-line shaped comb spectrum
The measured time-domain intensity autocorrelation traces of the 280 GHz pulse
Photonic MMW Source (IV)
FWHM 300fs ＜ 1ps
Notes: The figure shows the optical spectrum and 160GHz pulse.
So we could have Full-Width Half-Maximum 285fs much lower than 1 ps.

## Slide 38: Record-High Photo-Generated 124 GHz MMW Power: Optical MMW Short Pulse Source
15 dBm, 31 mW
Record-high MMW power (31 vs. 20 mW (UTC-PD))
MMW Power increases with number of comb lines (pulse width shortening)

## Slide 39
The breakthrough of NBUTC-PD:
Geometrical Structure of PD array
Optical MMW Source
Good Heat-Sinking for Sub-THz Operation

## Slide 40: cross-sectional view (after flip-chip bonding) of structures A and B
Heat-sinking
Speed
Heat-sinking
Speed
Yield
Signal
Signal
Maybe Yield

## Slide 41
Modeling Flip-Chip bonding structure
O-E bandwidth
Flip-Chip bonding structure has strong influence on O-E bandwidth!
Notes: Here shows the modeling result for PD which is bonding on the AlN structure. Flip-Chip bonding structure has strong influence on O-E bandwidth!

## Slide 42: Record Fastest PD (1.55 mm) …
Under 12.5 Ohm load: Poor output power
No reported saturation current
Low responsivity (<0.01 A/W)
InP/lnGaAs uni-travelling-carrier
photodiode with 310GHz bandwidth
Notes: １．很爛的輸出功率
２．沒說明飽和電流
３．很差的響應度

## Slide 43
Measured and modeling O-E bandwidth
Under low output photocurrent (3 mA), the optimum bias for maximum speed performance happens at -0.5 V. (“50 Ohm load”)
315GHz
300GHz
300GHz
when the output photocurrent reaches 8 mA, the optimum bias shifts to -1V (SCS effect) .
Further increase in reverse bias doesn’t help for speed and power
Notes: Under low output photocurrent (3 mA), the optimum bias for maximum speed (~315 GHz 3-dB bandwidth) performance happens at -0.5 V. On the other hand, when the output photocurrent reaches 8 mA, in order to compensate the electron induced SCS effect, the optimum bias shifts to -1V and the corresponding 3-dB bandwidth slightly degrades to 290 GHz.
GHz.

## Slide 44
Measured and modeling O-E bandwidth
Measured Bandwidth up to 315 GHz, ~0.1 A/W Responsivity
Optimum bias: -0.5~-1V (O-E f3dB > 315 GHz)
Notes: In the O-E bandwidth measurement, our 3 dB is up to 160 GHz.

## Slide 45
THz power measurement results
Enhancement (3.23 dB) in
high photocurrent operation regime: “Record high” output power for THz (~0.3 THz) bandwidth PD
12mA

## Slide 46
Significant Bias Dependent Speed Performance: Switch !!
Under reverse bias still has high nonlinearity!!
Very-high modulation speed!!
Without minority carrier injection under forward bias voltage

## Slide 47: High On/Off Ratio
>36dB
20dB
1.1V

## Slide 48: High On/Off Ratio
>36dB
Current doesn’t change during switching!!

## Slide 49: High On/Off Ratio
>36dB
A. Hirata, T. Furuta, H. Ito, and T. Nagatsuma, “10-Gb/s Millimeter-Wave Signal Generation Using Photodiode Bias Modulation,” J. of Lightwave Technol., vol. 24, pp. 1725–1731, April. 2006.
NTT’s UTC-PD
Forward
Best MMW Switch: High on/off ratio, Ultra-fast switching speed, low-driving voltage

## Slide 50
Outline
Introduction
Working Principle of NBUTC-PD
High-Power and Ultrafast Modulation Characteristic
Applications for MMW Over Fiber Communication
Conclusion

## Slide 51: Wireless Data Transmission

## Slide 52: Power Performance
Improved Power performance due to better Heat-sinking
18mA, 6.3dBm

## Slide 53: 25Gbit/s Wireless Data Transmission
Eye Height: 63mV Eye Width: 20ps
Error Free Performance!! (BER<1e-12)

## Slide 54: 25Gbit/s Wireless Data Transmission
This Work
25Gbit/s at 93GHz
Fraunhofer Institute for Applied Solid-State Physics(IAF)
15Gbit/s at 220GHz
NTT 48 Gbit/s at 300GHz
Highest Data Rate at Lowest Carrier Frequency!!

## Slide 55: Photonic MMW Short Pulse Generator
Beating Signal
Bias Modulation
Few Cycle MMW
Short Pulse
Not femtosecond Mode Lock Laser
Notes: Photonic MMW Short Pulse Generator

## Slide 56
Radar Imaging System
A.
B.
Detected Target
(Focus Point)
Receiver

## Slide 57
Resolution Measurement
Transmitting Horn
MMW Lens
Receiving Horn
Spot Size
Spatial Resolution
Temporal Resolution
1.053 cm

## Slide 58
Object Image Measurement
Object Under Test
Security Check
Envelope

## Slide 59
Object Image Measurement
Millimeter Wave Lens
Object Under Test
Receiving Horn Antenna
Transmitting Horn Antenna
Photonic Short
Pulse Generator

## Slide 60
Object Image Measurement

## Slide 61
Object Image Measurement

## Slide 62
Benchmark of MMW Radar Imaging
Table.1. Comparisons of Different MMW Radar Systems
[2] K. B. Widener, and J. B. Mead, “W-band ARM Cloud Radar-Specifications and Design” Fourteenth ARM Sci. Team Meeting Proc., Albuquerque, New Mexico, USA, March, 2004.
[3] P.-S Tsai, and S. Frasier, “The UMass Mobile W-band Radar: System Overview and Sample Observations” 24th Conference on Severe Local Storms, Savannah, Georgia, USA, June, 2008, P13.5
[4] R. W. McMillan, C. W. Trussell, Jr. R. A. Bohlander, J. C. Butterworth, and R. E. Forsythe, “An Experimental 225 GHz Pulsed Coherent Radar”, IEEE Trans. on Microwave Theory Tech., vol. 39, pp. 555-562, March, 1991.
[10] A. Y. Nashashibi, K. Sarabandi, P. Frantzis, R. D. De Roo, and F. T. Ulaby, “An Ultrafast Wide-Band Millimeter wave (MMW) Polarimetric Radar for Remote Sensing Applications”, IEEE Trans. on Geoscience and Remote Sensing, vol. 40, pp. 1777-1786, Aug., 2002.
[11] H. Essen, H.-H. Fuchs, M. Hagelen, S. Stanko, D. Notel, S. Erukulla, H. Huck, M. Schlechtweg, A. Tessmann, “Concealed Weapon Detection with Active and Passive Millimeterwave Sensors, Two Approaches” German Microwave Conference, Karlsruhe, Germany, March, 2006.
[12] H. Essen, S. Stanko, R. Sommer, W. Johannes, A. Wahlen, J. Wilcke, and S. Hantscher, “Millimeter Wave SAR for UAV Operation” Proc. Asian-Pacific Microwave Conference 2011, Melbourne, Australia, Dec., 2011, pp. 963-966.

## Slide 63
Outline
Introduction
Working Principle of NBUTC-PD
High-Power and Ultrafast Modulation Characteristic
Applications for MMW Over Fiber Communication
Conclusion

## Slide 64: Conclusion
Higher optimum bias for near-ballistic transport in NBUTC-PD : p-type (or n-type) charge layer in collector
Record high output power for PD with THz bandwidth (0.3 THz)
Ultra-fast switching characteristic: Field-effect to modulate electron drift-velocity (good MMW switch !!)
High Performance photonic-transmitter mixer: Good PD modeling and MMW design
State-of-the-art resolution of photonic radar system has been demonstrated
Very-High error-free wireless data rate (25 Gbps) with high-power performance (~ 20mA) saturation current)

## Slide 65
Thanks for your attention !!